AAT48160. DH AL/AL TRIFIRM RIVET 4.8*16.0 mm.

Batch no. 20230318. Order-No.:123456. Quantity: 532.000pcs.

Test no. 1, measurements test.

The dimension of ‘d’ should be 4.95mm max.

Test no.2, grip range test with lower grip range1.0mm.

The rest mandrel is deeply inside after setting test with hole size 5.0mm, all of 5 samples are found.

The rest mandrel is deeply inside after setting test with hole size 5.2mm, all of 5 samples are found.

Test no.3, grip range test with upper grip range 4.0mm.

The rest mandrel is deeply inside after setting test with hole size 5.0mm, all of 5 samples are found.

The rest mandrel is deeply inside after setting test with hole size 5.2mm, all of 5 samples are found.

Test no. 4, mandrel retaining test.

Test no. 5, shearing test.

Required  value:750N

Test no. 6, tensile test.

Required  value:950N

Test no. 7, mandrel breaking test.

| Test report samples |  |
| --- | --- |
| Supplier | Rivmate |
| Description | Tri-firm |
| Code | AAT488160 |
| Batch (Lot no) | 20230318 |
| Checked by |  |
| Date | 23.07.21 |

| Test No 1 Measurements |  | Used calliper no. |  |
| --- | --- | --- | --- |
|  |  | Mitutoyo WS-SXKC-086 |  |
|  | Reference | Result | Picture |
| d | Max. 4.95 mm | 4.79 4.78 4.75 4.76 4.76 |  |
| dk | Max. 10.10 mm | 9.81 9.87 9.81 9.96 9.88 |  |
| k | Max. 2.10 mm | 1.83 1.87 1.82 1.85 1.86 |  |
| dm | Max. 2.90 mm | 2.86 2.86 2.87 2.90 2.90 |  |
| P | Min. 27.00 mm | 27.81 27.93 27.96 27.81 27.90 |  |
| L | Nom. 15.7-16.8 mm | 16.19 16.21 16.14 16.34 16.31 |  |

| Test No 2 Grip range test | Steel washer, thickness of material 1.00mm/hole size of test washers 5.00mm | Steel washer, thickness of material 1.00mm/hole size of test washers 5.20mm | Picture |
| --- | --- | --- | --- |
| Under grip range |  |  |  |
| Item 1 | Ok | Ok |  |
| Item 2 | Ok | Ok |  |
| Item 3 | Ok | Ok |  |
| Item 4 | Ok | Ok |  |
| Item 5 | Ok | Ok |  |
| Test result (notes) |  |  |  |

| Test No 3 Grip range test | Steel washer, thickness of material 4.00mm/hole size of test washers 5.00mm | Steel washer, thickness of material 4.00mm/hole size of test washers 5.20mm | Picture |
| --- | --- | --- | --- |
| Upper grip range |  |  |  |
| Item 1 | Ok | Ok |  |
| Item 2 | Ok | Ok |  |
| Item 3 | Ok | Ok |  |
| Item 4 | Ok | Ok |  |
| Item 5 | Ok | Ok |  |
| Test result (notes) |  |  |  |

| Test No 4 Retaining mandrel | Steel washer, thickness of material 1.00mm/hole size of test washers 5.00mm | Steel washer, thickness of material 1.00mm/hole size of test washers 5.20mm | Picture |
| --- | --- | --- | --- |
| Grip range |  |  |  |
| Item 1 | 794 | 758 |  |
| Item 2 | 725 | 726 |  |
| Item 3 | 775 | 798 |  |
|  | Steel washer, thickness of material 4.00mm/hole size of test washers 5.00mm | Steel washer, thickness of material 4.00mm/hole size of test washers 5.20mm |  |
| Item 1 | 772 | 749 |  |
| Item 2 | 915 | 765 |  |
| Item 3 | 768 | 791 |  |
| Test result (notes) |  |  |  |

| Test No 5 Shearing strength ISO 14589 |  |  | Picture |
| --- | --- | --- | --- |
| Grip range | Tool thickness of material 3.00mm / hole size of test tool 5.20mm | Ref data sheet |  |
| Item 1 | 1053 | Min 750 N |  |
| Item 2 | 1068 | Min 750 N |  |
| Item 3 | 1055 | Min 750 N |  |
| Item 4 | 1024 | Min 750 N |  |
| Item 5 | 1094 | Min 750 N |  |
| Test result (notes) |  |  |  |
| Details of testing Machine for Test No. 5 | Diameter |  |  |
| Test tool no. | 5.20 x 1.50 mm |  |  |
| Test tool no. | 5.20 x 1.50 mm |  |  |

| Test No 6 Tensile strength ISO 14589 |  |  | Picture |
| --- | --- | --- | --- |
| Grip range | Tool thickness of material 3.0mm / hole size of test tool 5.2mm | Ref data sheet |  |
| Item 1 | 1474 | Min. 950 N |  |
| Item 2 | 1492 | Min. 950 N |  |
| Item 3 | 1468 | Min. 950 N |  |
| Item 4 | 1415 | Min. 950 N |  |
| Item 5 | 1345 | Min. 950 N |  |
| Test result (notes) |  |  |  |
| Details of testing machine for Test No. 6 | Diameter |  |  |
| Test tool no. | 5.20 x 1.50 mm |  |  |
| Test tool no. | 5.20 x 1.50 mm |  |  |

| Test No 7 Mandrel breaking test ISO 14589 |  | Picture |
| --- | --- | --- |
|  | Result |  |
| Item 1 | 1790N |  |
| Item2 | 1840N |  |
| Item 3 | 1810N |  |
| Test result (notes) |  |  |